SPECIFICATIONS

# Br 250 Level 3 Curtain Wall

## General Description

Work included: Furnish all necessary materials, labor, and equipment for the complete installation of aluminum door and framing as shown on the drawings and specified herein (it is recommended that specifier include related items, i.e.: glass sealants, entrances, etc. when possible.)  All framing members shall conform to the exact profiles, and configurations.

Work not included: Structural support of the framing system, aluminum sub sills, flashing, receptors, closures.  (Other exclusions by specifier)

Related Work: (see specifier list)

## Quality Assurance

Drawings and specifications are based on BR 250 Curtain Wall system as manufactured by Action Bullet Resistant, Inc.

Other manufacturers requesting approval to bid their products as an equal must submit the following information fifteen days prior to closing of bidding.

- Test reports by a certified test lab showing compliance with UL 752 standards to meet threat level 3.

- A sample window (specifier to determine sample size) as per architects requirements.

(It is recommended that specifier specify glass and glazing in section 08800.  Action recommends that the window manufacturer provide the glazing if specified in this section.)

Curtain Wall Construction

- Aluminum Extrusions: shall be extruded from prime billet.  Alloy and temper to be equivalent to 6005-T5 (Tensile strength- ksi with a minimum ultimate of 38.0 and minimum yield of 35.0).

- Heavy-duty aluminum bullet resistant in itself without the need for bullet resistant filler material.

- Frame to be 2 ½” x 4 ½” with 3/16” minimum wall thickness on vertical mullion and 3/32” minimum wall thickness on horizontal mullion.

- Glazing pocket to be 1” deep for proper bite.

- Glazing gasket to be neoprene.

- Frames to have screw spline system with tight hairline joints where horizontal mullions meet vertical mullions.

(Finishes as specified on drawings.)

Window Glazing

- Bullet resistant glazing shall be specified by the end user consistent with threat level 3.

- Glazing material for bullet resistant use shall be of a type listed by Underwriters Laboratories standard 752 for bullet resistance and or as approved by H.P.White Test Laboratories for specified bullet resistance.

## Limitations

Action Bullet Resistant, Inc., BR 250 Curtain Wall window is designed to meet the UL standard 752-threat level 3.  It is recommended that each end-user determine their ballistic threat and identify the correct product to resist that threat.