AMERISTAR® PERIMETER SECURITY USA INC.

MATRIX® – Perimeter Enclosure Grid (PEG) Framing System

Construction Specification – SECTION 32 31 00

PART 1 - GENERAL

1.01    WORK INCLUDED

The contractor shall provide all labor, materials and appurtenances necessary for installation of the industrial steel perimeter enclosure grid fence system defined herein at (specify project site).

1.02    RELATED WORK

Section ___  ___  -  Earthwork

Section ___  ___  - Concrete

1.03    SYSTEM DESCRIPTION

The manufacturer shall supply a steel perimeter enclosure grid framing system of the Matrix® design, (specify mesh filler, Table 3) style.  The system shall include all components (i.e., mesh filler, retainer channels, rails, posts, gates and hardware) required.

1.04    QUALITY ASSURANCE

The contractor shall provide laborers and supervisors who are thoroughly familiar with the type of construction involved and materials and techniques specified.

1.05 REFERENCES

- ASTM A653/A653M - Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy Coated (Galvannealed) by the Hot-Dip Process.

- ASTM B117 - Practice for Operating Salt-Spray (Fog) Apparatus.

- ASTM B221 - Standard Specification for Aluminum and Aluminum-Alloy Extruded Bars, Rods, Wire, Profiles and Tubes.

- ASTM D714 - Test Method for Evaluating Degree of Blistering in Paint.

- ASTM D1654 - Test Method for Evaluation of Painted or Coated Specimens Subjected to Corrosive Environments.

- ASTM D2794 - Test Method for Resistance of Organic Coatings to the Effects of Rapid Deformation (Impact).

- ASTM D3359 - Test Method for Measuring Adhesion by Tape Test.

- ASTM F2548 – Expanded Metal Fence Systems for Security Purposes.

- ASTM F2453/F2453M – Welded Wire Mesh Fence Fabric…

- ASTM F2781 – Testing Forced Entry, Ballistic and Low Impact Resistance of Security Fence Systems

- IEEE P80/D10 Draft Guide for Safety in AC Substation Grounding

- IEEE 142-1991 IEEE Recommended Practice for Grounding of Industrial and Commercial Power Systems

- IEEE 81-2012 IEEE Guide for Measuring Earth Resistivity, Ground Impedance, and Earth Surface Potentials for a Ground System

- UL 752 Ballistic Standards

1.06    SUBMITTAL

The manufacturer's submittal package shall be provided prior to installation.

1.07    PRODUCT HANDLING AND STORAGE

Upon receipt at the job site, all materials shall be checked to ensure that no damage occurred during shipping or handling. Materials shall be stored in such a manner to ensure proper ventilation and drainage, and to protect against damage, weather, vandalism and theft.

1.08 PRODUCT WARRANTY

All structural fence components (i.e. rails and I-beam posts) shall be warranted within specified limitations, by the manufacturer for a period of 10 years from date of original purchase.  Warranty shall cover any defects in material finish, including cracking, peeling, chipping, blistering, or corroding.  Matrix is also guaranteed for the same period of time against defects in workmanship or materials.  See product specific warranty for additional details.

1.09 PRODUCT TESTING & COMPLIANCE

A.  Fence system shall be tested by third party professional engineer to IEEE P80/D10, IEEE 142-1991 and IEEE 81-2012.  Test report shall be supplied showing fence system meeting acceptable range for resistance and impedance required within the IEEE standards listed here within.

B.  Fence system shall be tested to ASTM standard F2781 for forced entry by third party certified testing organization.  Test summary documentation shall be made available upon request.

C.  If ballistic resistant in-fills are required material shall meet UL 752 standards Level 3 thru Level 8 protection.

PART 2 - MATERIALS

2.01	MANUFACTURER

The fence system shall conform to perimeter enclosure grid framing system of the Ameristar Matrix design, (specify mesh filler, Table 3) style, manufactured by Ameristar Perimeter Security USA Inc. in Tulsa, Oklahoma.

2.02	MATERIAL

A.  Steel material for perimeter enclosure grid framework (i.e. rails and I-beam posts), shall have a minimum yield strength of 45,000 psi (310 MPa).  The steel shall be hot-dip galvanized to meet the requirements of ASTM A653/A653M with a minimum zinc coating weight of 0.90 oz/ft2 (276 g/m2), Coating Designation G-90.

B.  The cross-sectional shape of the rails shall conform to the manufacturer's Matrix “C” shaped rail design a nominal 2” x 2” x 11 Ga.  Matrix rail shall be pre-drilled to accept fasteners for attachment of mesh retainer channel.  Fence posts shall meet the minimum system requirements.

C. The cross-sectional shape of the mesh retainer channels shall conform to the manufacturer’s channel design with outside cross-section nominal dimensions of 3.5” x .75” (channel dimensions vary to match optional ballistic resistant fillers).  Aluminum material for channel & cap shall conform to the requirements of ASTM B221, alloy designation 6005-T5 & 6063-T5.

D. Matrix mesh filler material shall comply with one of the options listed in Table 3.

2.03    FABRICATION

A.  Rails and I-beam posts shall be pre-cut to specified lengths.  Matrix rails shall be pre-punched to accept security fasteners.  Post flange shall be pre-punched to accept rail to I-beam post attachment.  I-beam posts shall be pre-punched providing a source for attachment of conduits to interior post flange.  Post web shall be punched providing a clear opening for interior of rails to align throughout the entire system for affixing conduit, video cabling, IDS (Intrusion Detection System) wiring, and other components for a complete systems integration.  Matrix rails shall be attached to post flange providing a bracket-less design at each intermediate post.

B.  Mesh retainer channels shall be precut to specified lengths.  Mesh retainer channels shall be affixed horizontally to rails to accommodate the insertion of specified filler material.  Locking cover shall be introduced onto the channel to conceal and secure mesh retainer channel fasteners.

C.  Filler panels shall be inserted into the mesh retainer channels to conceal and secure filler material to the framework.  Filler material shall be affixed to I-beams using appropriate filler attachment brackets and fasteners.

D.  Integrated technology post shall be pre-manufactured with access ports strategically located and have predrilled holes for attachment.  Technology post base shall be a minimum 6” x 6” square, and either 18 or 20 feet above grade.

E.  Swing gates shall match style, height, and color of fence system.  All rail and upright intersections shall be joined by welding.

Mesh filler shall be securely affixed to gate frame by welding.

F.  Sliding cantilever gates shall match fence system.  Slide gate shall be an aluminum component design using enclosed tracks, uprights, mesh filler, hardware, fittings, and fasteners.  Gate installation shall comply with latest ASTM F2200 standards for automated gates.

G.  Pedestrian swing gates shall match fence system.  Gate shall be pre-drilled to accept appropriate hardware set.  Infill frames shall be fabricated as a single unit.  Frame shall be of welded construction inset with mesh filler, attachment to gate frame by means of security fasteners.  Gate jamb frame shall be fully welded consisting of 3” x 12ga square tubing for main jamb, 1” square gate stop, and strike mounting block, with gate stop bumpers.  Jamb to include an electrical access point with conduit point of connection.  Electrical connection to gate by means of Power Transfer connection mounted in jamb and gate.  Gate shall be pre-assembled.  Gate threshold to be mounted with fasteners allowing for placement below grade or removal after gate installation.  Gate hardware to consist of exterior rated devices.  Gate and hardware to be pre-assembled prior to shipping.  Gate opening shall be designed to accommodate a 48” clear opening.

H.  Optional – Animal mitigation shield shall be securely mounted to top portion of fence and gate system.  Animal shield shall provide positive deterrent from nuisance animals intruding into protected areas.  System shall be installed along the upper most portion of the fence and gate system and throughout the entire perimeter including all corners and/or changes in fence direction.  Animal mitigation system shall be evaluated and recommended by an accredited herpetologist for mitigating intrusion of nuisance animal’s i.e. snakes, raccoons, squirrels, iguanas, rodents of unusual size, possums, cat species & nutria.

I.  Optional – Barbwire deterrent shall be installed at top of fence and gate system.  Barbwire deterrent shall have a minimum of 3 strands and be affixed to barb arms.  Barb arms shall be securely attached to each line and terminal posts.

J.  Optional –Spike Deterrent Strips shall be securely attached to the top of fence and gate system.  Spike Deterrent strips shall be 12ga. (.075”) galvanized steel, spike sets shall alternate between two heights every 2 inches, spike set heights shall be 2.75 inches and 3.5 inches.  Spike deterrent strips shall affix atop fence and gate system not exceeding a distance between each strip section of 2 inches.

PART 3 - EXECUTION

3.01    PREPARATION

All new installation shall be laid out by the contractor in accordance with the construction plans.

3.02 FENCE INSTALLATION

Fence post shall be spaced according to Table 1.  Fence framework and mesh filler shall be attached to system posts with fasteners supplied by the manufacturer.  Posts shall be installed as noted in Post Selection Table (Note:  In some cases, local restrictions of freezing weather conditions may require a greater depth).  The “Earthwork” and “Concrete” sections of this specification shall govern material requirements for the concrete footer.  Posts setting by other methods such as plated posts or grouted core-drilled footers are permissible only if shown by engineering analysis to be sufficient in strength for the intended application.

3.03 FENCE INSTALLATION MAINTENANCE

When cutting/drilling steel and aluminum system components adhere to the following steps to seal the exposed surfaces; 1) Remove all metal shavings from cut area.  2) Apply zinc-rich primer to thoroughly cover cut edge and/or drilled hole; let dry.  3) Apply 2 coats of custom finish paint matching fence color.  Failure to seal exposed surfaces per steps 1-3 above will negate warranty.  Ameristar spray cans or paint pens shall be used to prime and finish exposed surfaces; it is recommended that paint pens be used to prevent overspray.  Use of non-Ameristar parts or components will negate the manufactures’ warranty.

3.04 GATE INSTALLATION

Gate posts shall be spaced according to the manufacturers’ gate drawings, dependent on standard out-to-out gate leaf dimensions and gate hardware selected.  Type and quantity of gate hinges shall be based on the application; weight, height, and number of gate cycles.  The manufacturers’ gate drawings shall identify the necessary gate hardware required for the application.  Gate hardware shall be provided by the manufacture of the gate and shall be installed per manufacturer’s recommendations.

3.05 CLEANING

The contractor shall clean the jobsite of excess materials; post-hole excavations shall be scattered uniformly away from posts.

| Table 1 – Matrix Post Setting On Level Grade |
| --- |
| Post Type | Level Line | Level Corner | Tech Post Line | Tech Post Corner |
| Level Line | 95.75” | 96” | 97.25” | 97.125” |
| Level Corner | 96” | 96.25” | 97.5” | 97.375” |
| Tech Post Line | 97.25” | 97.5” | 98.75” | 98.625” |
| Tech Post Corner | 97.125” | 97.375” | 98.625” | 98.5” |
| Matrix Post Setting Un-Level Grade |
|  | Uphill Post |
| Post Type | Buried Line | Buried Corner | Plated Line | Plated Corner | Tech Post Line | Tech Post Corner |
| Downhill Post | Buried Line | 97.25” | 96” | 95.75” | 96” | 97.25” | 97.125” |
|  | Buried Corner | 97.5” | 96.25” | 96” | 96.25” | 97.5” | 97.375” |
|  | Plated Line | 98.5” | 97.5” | 97.25” | 97.5” | 98.75” | 98.625” |
|  | Plated Corner | 97.5” | 96.625” | 96” | 96.25” | 97.5” | 97.375” |
|  | Tech Post Line | 98.75” | 97.5” | 97.25” | 97.5” | 98.75” | 98.625” |
|  | Tech Post Corner | 98.625” | 97.375” | 97.125” | 97.375” | 98.625” | 98.5” |

| Table 2 – Coating Performance Requirements |
| --- |
| Quality Characteristics | ASTM Test Method | Performance Requirements |
| Adhesion | D3359 – Method B | Adhesion (Retention of Coating) over 90% of test area (Tape and knife test). |
| Corrosion Resistance | B117, D714 & D1654 | Corrosion Resistance over 3,500 hours (Scribed per D1654; failure mode is accumulation of 1/8” coating loss from scribe or medium #8 blisters). |
| Impact Resistance | D2794 | Impact Resistance over 60 inch lb. (Forward impact using 0.625” ball). |

| Table 3 – Matrix Filler Options |
| --- |
| Trade Name | Product | Description | Screening |
| X-Span™ | Expanded Metal Mesh | .5" x #13R (.188 strand width) Modified - ASTM F2548 | 75% screening |
|  |  | .75" x #9F - ASTM F2548 | 37% screening |
| X-Screen™ | Louvered Mesh (Steel) | 1.5” x #14 | 94% screening |
| WireWorks™ | Welded Wire Mesh | .5" x 3" x 8ga. - ASTM F2453/F2453M | 37% screening |
|  |  | .5" x 3" x 6ga. - ASTM F2453/F2453M | 43% screening |
|  | Ballistic Resistant Panel | UL 752 standards Level 3 thru Level 8 protection | 100% screening |