AMERISTAR FENCE PRODUCTS

TRANSPORT IS – Enclosed Track Industrial Aluminum Cantilever Gate System

Construction Specification – SECTION 32 31 00

PART 1 - GENERAL

1.01 WORK INCLUDED

The contractor shall provide all labor, materials, and appurtenances necessary for installation of the industrial cantilever gate system defined herein at (specify project site).

1.02 RELATED WORK

Section _____ _____ - Earthwork

Section _____ _____ - Concrete

1.03 SYSTEM DESCRIPTION

The manufacturer shall supply a total industrial ornamental aluminum cantilever gate system of the Ameristar® TransPort IS design, (specify Stronghold, Trident, or Gauntlet) style.  The system shall include all components (i.e., tracks, uprights, bracing, pickets, hardware, fittings and fasteners) required.

1.04 QUALITY ASSURANCE

The contractor shall provide laborers and supervisors who are thoroughly familiar with the type of construction involved and materials and techniques specified.

1.05 REFERENCES

ASTM B117 - Practice for Operating Salt-Spray (Fog) Apparatus.

ASTM B221 - Aluminum and Aluminum-Alloy Extruded Bars, Rods, Wire, Profiles and Tubes.

ASTM D523 - Test Method for Specular Gloss.

ASTM D822 - Practice for Conducting Tests on Paint and Related Coatings and Materials using Filtered Open-Flame Carbon-Arc Light and Water Exposure Apparatus.

ASTM D1654 - Test Method for Evaluation of Painted or Coated Specimens Subjected to Corrosive Environments.

ASTM D2244 - Test Method for Calculation of Color Differences from Instrumentally Measured Color Coordinates.

ASTM D2794 - Test Method for Resistance of Organic Coatings to the Effects of Rapid Deformation (Impact).

ASTM D3359 - Test Method for Measuring Adhesion by Tape Test.

ASTM F1184 – Industrial & Commercial Horizontal Slide Gates

1.06 SUBMITTAL

The manufacturer’s submittal package consisting of gate elevations, hardware details, and installation details, shall be submitted prior to installation.

1.07 PRODUCT HANDLING AND STORAGE

Upon receipt at the job site, all materials shall be checked to ensure that no damage occurred during shipping or handling.  Materials shall be stored in such a manner to ensure proper ventilation and drainage, and to protect against damage, weather, vandalism, and theft.

PART 2 - MATERIALS

2.01 MANUFACTURER

All industrial ornamental aluminum cantilever gates shall conform to the Ameristar® TransPort IS gate system, (specify Stronghold, Trident, or Gauntlet) style, manufactured by Ameristar Fence Products, Inc., in Tulsa, Oklahoma. The project gate schedule shall include the following additional information for each cantilever gate included in the project scope: (specify nominal opening size range in feet) opening, and (specify size and shape of posts) gate posts.

2.02 MATERIAL

A.  The materials used for cantilever gate framing (i.e., uprights, diagonal braces and pickets or pales) shall be manufactured from ASTM B221 aluminum (designation 6063-T-6) with a yield strength of 25,000 PSI, a tensile strength of 30,000 PSI and a standard mill finish. The TransPort® Fast-Trak™ rails shall be manufactured from ASTM B221 aluminum (designation 6063-T-6) with minimum yield strength of 25,000 PSI, a tensile strength of 30,000 PSI and a standard mill finish.

B. Material for diagonal bracing and uprights shall be 2” sq. x ¼” aluminum.  The design of the top and bottom enclosed track shall conform to the manufacturers 5” x 2” Fast-Trak system.  Material for pales shall be 2.75” x 1/8” wall aluminum.

C.  Internal roller truck assembly shall be self-aligning swivel ball-and-socket type running on four bearing wheels.  Internal roller truck assembly shall be affixed to the hanger bracket by means of a 5/8” diameter industrial-grade rod end/center bolt, with a minimum static load rating of 10,000 pounds.  Attachment of the center bolt to the truck body shall be by means of a swivel joint to ensure equivalent and consistent loading on all bearing wheels and internal track surfaces throughout the travel of the gate.

2.03 FABRICATION

A. Pickets, enclosed track, uprights and diagonal bracing shall be pre-drilled and labeled for easy assembly.  All components shall be precut to specified lengths.

B. Top and bottom rail extrusions shall be mechanically fastened to vertical uprights and reinforced with diagonal braces, as required by drawing.

C.  The manufactured components shall be subjected to the Ameristar thermal stratification coating process (high-temperature, in-line, multi-stage, and multi-layer) including, as a minimum, a six-stage pretreatment/wash and an electrostatic spray application of a polyester finish. The topcoat shall be a “no-mar” TGIC polyester powder coat finish with a minimum thickness of 2 mils (0.0508mm). The color shall be (specify Black, Bronze, White, or Desert Sand). The stratification-coated framework shall be capable of meeting the performance requirements for each quality characteristic shown in Table 1.

| Table 1 – Coating Performance Requirements |
| --- |
| Quality Characteristics | ASTM Test Method | Performance Requirements |
| Adhesion | D3359 – Method B | Adhesion (Retention of Coating) over 90% of test area (Tape and knife test). |
| Corrosion Resistance | B117, D714 & D1654 | Corrosion Resistance over 3,500 hours (Scribed per D1654; failure mode is accumulation of 1/8” coating loss from scribe or medium #8 blisters). |
| Impact Resistance | D2794 | Impact Resistance over 60 inch lb. (Forward impact using 0.625” ball). |
| Weathering Resistance | D822 D2244, D523 (60˚ Method) | Weathering Resistance over 1,000 hours (Failure mode is 60% loss of gloss or color variance of more than 3 delta-E color units). |

PART 3 - EXECUTION

3.01 PREPARATION

A.  All new gate installations shall be laid out by the contractor in accordance with the construction plans.

B.  All hardware shall be installed in accordance with the Transport installation instructions.  Transport cantilever gates shall be installed so they comply with current ASTM F2200 & UL325 standards.

C.  Gate stops shall be installed on each track in a way that conforms to current ASTM F2200 standards.

3.02 GATE INSTALLATION

Gate post shall be spaced according to specified gate elevation.  Posts shall be set in concrete footers having a minimum depth of 48” with a minimum diameter of 12” (Note: In some cases, local restrictions of freezing weather conditions may require a greater depth). The “Earthwork” and “Concrete” sections of this specification shall govern material requirements for the concrete footer. Posts setting by other methods such as plated posts or grouted core-drilled footers are permissible only if shown by engineering analysis to be sufficient in strength for the intended application.

3.03 CLEANING

The contractor shall clean the jobsite of excess materials; post-hole excavations shall be scattered uniformly away from posts.